## Fire Resistant and Thermally Stable Materials Derived from Chlorinated Polyethylene

New Concepts in Polymer Science

### Contents:

Preface

Introduction

COMBUSTION OF POLYMERIC MATERIALS AND METHODS TO REDUCE IT. THE MECHANISM OF FIRE AND HEAT SHIELD COVERS

INVESTIGATION METHODS FOR FIRE AND HEAT SHIELD MATERIALS AND COVERS BASED ON THEM

CHLORINATED POLYMERS AS THE BASE FOR MATERIALS WITH REDUCED COMBUSTIBILITY

Current state of chlorinated polyolefins production and application

Chlorination methods; Structure and properties

VULCANIZATION

Vulcanization effect on physical and mechanical properties and stability of materials

Study of vulcanization mechanism and the effect of fillers

FILLERS

Inorganic fillers and their function in decreasing combustibility

Organic compounds increasing fire shield properties of materials

Combustion decelerators. Operation mechanism and injection methods

Methods of antipyren injection into materials

Application of phosphorus-containing compounds on the silicon dioxide surface from the liquid phase

Obtaining of phosphorus-containing silica filler by mechanochemical method

Study of biological activity of phosphorus-containing silicon dioxides

Study of fire and heat shield properties of materials filled with modified silicon dioxide

PLASTICIZERS

Influence of plasticizers on glass transition temperature and flow rate of polymers

Classification of plasticizers

Selection of plasticizers

Miscibility of plasticizers with polymers; Plasticizer effect on mechanical, fire and heat shield, and electrical properties of composite materials

TESTS OF MATERIALS. STUDY OF OPERATION MECHANISM AT HIGH-TEMPERATURE INFLUENCE

Coke formation as the investigation method of fire and heat shield materials and covers

The role of intumescence in the problem of fire protection of polymers

Intumescence chemistry; Protection through intumescence; The role of ammonium polyphosphates in protection of polymers from fire

DEVELOPMENT OF FIRE AND HEAT SHIELD MATERIALS

CLIMATIC NATURAL AND ARTIFICIAL AGING OF MATERIALS

MULTILAYER MATERIALS FOR INCREASING EFFICIENCY OF COVERS

Materials with surface reinforcement

Heat-accumulating materials in cover compositions

Estimation of thermophysical properties of heat-accumulating materials

TESTS OF MATERIALS AS COVERS FOR FLIGHT INFORMATION RECORDERS UNDER CONDITIONS MODELING AN ACCIDENT

Conclusion

References

Subject Index