Comparison between FRIPP’s MEK technology and reference MEK technology

| Item | FRIPP technology | Reference technology |
| --- | --- | --- |
| Hydration process |  |  |
| Butene concentration feedstock, % | 97 | 97 |
| Operating temperature, ℃ | 135-175 | 145-175 |
| Operating pressure, MPa | 6.0-7.0 | 6.0 |
| LHSV, h-1 | 1.0-1.3 | 1.5 |
| Water/n-butene molecular ratio | 1.60-2.05 | 1.0 |
| Single pass conversion of n-butene, mol% | 8.0-11.0 | 6.0 |
| Total conversion of n-butene, mol% | 90 | 80 |
| Selectivity of secondary vinyl alcohol to n-butene, mol% | 98 | 93 |
| Butene recycling ratio | 10.3 | 12.3 |
| Catalyst volume, M3 | 23.3 | 22 |
| Dehydrogenation process |  |  |
| Operating temperature, ℃ | 260 | 260 |
| Operating pressure, MPa | 0.1 | 0.2 |
| LHSV, h-1 | 3.6-4.0 | 4.0 |
| Conversion of secondary butyl alcohol, mol% | 86.7 | >80 |
| Selectivity to MEK, mol% | 96.6 | >95 |
| Catalyst life | >3500 hrs | 6-8 weeks |