Table 3 Main Properties of Hot-melt Adhesive

| Item | Properties |
| --- | --- |
| Appearance | White powder |
| point,℃ | 110-120 |
| Melt index(150℃,2.15kg),g/10min | 16 |
| Peeling strength (kgf/2.5) | 11 |
| Washing peeling strength (kgf/2.5) | 6.0 |
| Dry-clean peeling strength (kgf/2.5) | 6.4 |